厦门迪太进出口有限公司

XIAMEN DITAI IMP.& EXP. CO.,LTD

地址：中国厦门禾祥西路鸿升大厦8A

8FL, Hongsheng Building, West Hexiang Road, Xiamen, Fujian, China

TEL:0592-26808108 FAX:0592-2680880 E-mail: irene.zhang@xmditai.com

Sodium Metasilicate 5H2O CAS 10213-79-3

Sodium Silicate

Applications: Sodium Silicate is mainly used in the industries of paper, soap, detergent, construction materials, delicate casting, anti corrasion material, textile, and mineral floating select. And it is primary raw material of silicon rubber, silicon aluminum rubber, moisture absorbent, catalyst and its carrier, desalt agent of brine, hydrated silica and absorbent.

​

Specification:

1) Sodium Silicate glass 98.5min(Neutral grade)

| Parameter | Specification |
| --- | --- |
| Molar ratio | 3.0-3.5 |
| Na2O | 22 - 22.5% |
| SiO2 | 73 - 76.5% |
| Fe | 0.03% max |
| Soluble matter: | 98.5%min |

2) Sodium Silicate glass 98.5%MIN (Alkaline grade)

| Parameter | Specification |
| --- | --- |
| Molar ratio | 1.9-2.5 |
| Na2O | 28 - 35% |
| SiO2 | 68.5 - 70.5% |
| Fe | 0.03% max |
| Soluble matter: | 98.5%min |

Classification: Silicate

Type: Sodium Silicate

Other Names: water glass
CAS No.: 1344-09-8
HS CODE: 28391910
Molecular Formula: Na2O*mSiO2

Place of Origin:  Shandong, China (Mainland)

Purity:98.5% Min

Color:    Translucence Color
Packaging Details: Packing: 1MT/1.1MT/1.2MT/1.25MT JUMBO BAG
Delivery Detail: prompt shipment