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Sodium Metasilicate 5H2O CAS 10213-79-3

   
     
Sodium Silicate
Applications: Sodium Silicate is mainly used in the industries of paper, soap, detergent, construction materials, delicate casting, anti corrasion material, textile, and mineral floating select. And it is primary raw material of silicon rubber, silicon aluminum rubber, moisture absorbent, catalyst and its carrier, desalt agent of brine, hydrated silica and absorbent.
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Specification:
1) Sodium Silicate glass 98.5min(Neutral grade)
	Parameter
	Specification

	Molar ratio
	3.0-3.5

	Na2O
	22 - 22.5%

	SiO2
	73 - 76.5%

	Fe
	0.03% max

	Soluble matter:
	98.5%min


 





[bookmark: _GoBack]2) Sodium Silicate glass 98.5%MIN (Alkaline grade)
	Parameter
	Specification

	Molar ratio
	1.9-2.5

	Na2O
	28 - 35%

	SiO2
	68.5 - 70.5%

	Fe
	0.03% max

	Soluble matter:
	98.5%min


 
Classification: Silicate
Type: Sodium Silicate
Other Names: water glass
CAS No.: 1344-09-8
HS CODE: 28391910
Molecular Formula: Na2O*mSiO2
Place of Origin:  Shandong, China (Mainland)
Purity:98.5% Min
 
Color:    Translucence Color
Packaging Details: Packing: 1MT/1.1MT/1.2MT/1.25MT JUMBO BAG
Delivery Detail: prompt shipment
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